## Slide 1: FE Exam Civil CBT Specifications Section 7 - Materials

## Slide 2: Review on Civil Engineering Materials
Aggregates
Portland Cement Concrete
Asphalt Concrete
Steel
Wood

## Slide 3: Aggregates

## Slide 4: Classification of Aggregates
Based on Origin (Natural & Artificial)
Based on Density of Particles
  Normal Weight (SG 2.5-2.8); Light Weight (SG 1.5-2.0)
Based on Method of Processing
Based on Affinity to Water
  Hydrophilic (siliceous); Hydrophobic (Carbonaceous)
Based on Particle Size
  Coarse Aggregate (Larger than #4 sieve)
  Fine Aggregate: #4(4.75mm) to #200 sieves (75 m)
  Mineral filler (finer than #200 sieve)
Uncrushed
Crushed

## Slide 5: Natural & Artificial Aggregate Types
Natural aggregates from:
Igneous Rocks (Granite, Basalt)
Metamorphic Rocks (Marble, Gneiss, Quartzite)
Sedimentary Rocks (Limestone, Dolomite, Sandstone, Caliche)
Artificial aggregates from:
Byproducts of Industrial Processes (Blast-furnace slag; Iron-ore gravel)
Manufactured Aggregates (Lightweight aggregate, Hydrated fly ash)

## Slide 6: Important Aggregate Properties
Gradation (ASTM C-33)
Specific Gravity & Absorption (ASTM C-127, C-128)
Durability
  Physical Durability
    Abrasion Resistance (LA Abrasion Test: ASTM C131)
    Frost Resistance (Soundness Test: ASTM C88)
  Chemical Durability
    Alkali-aggregate reactivity (in Portland CC)
Shape and Surface Texture
Deleterious Substances (ASTM C-40, C-142)
Standard Tests by ASTM, AASHTO, State DOTs

## Slide 7: Aggregate Gradations
Continuous
Gap
Uniform

## Slide 10: Aggregate Moisture States

## Slide 11: Absorption & Surface Moisture
PCA

## Slide 12: LA Abrasion Test
Before
After
(Uses #12 Sieve)
Soundness Test
Before
After
(Uses 8mm Sieve)
  Five cycles of
  Soaking (in Mg or Sodium Sulfate solution),
  Oven Drying

## Slide 13: Portland Cement Concrete

## Slide 14: Constituents of Portland Cement Concrete
Cementitious Materials
  Portland cement
  Mineral admixtures or supplemental cementitious materials (i.e. fly ash, slag, silica fume)
Water
  For hydration
  For Workability
Aggregates
  Coarse aggregate
  Fine aggregate
Air Voids
Chemical admixtures

## Slide 15: Constituents of Portland Cement Concrete
Portland Cement Concrete (PCC)
Mortar
Coarse Aggregate
Fine Aggregate (Sand)
Cement Paste
Cementitious Materials
Water
Air
Chemical Admixtures
Portland Cement
Supplementary
Cementitious Materials,
aka Mineral Admixtures
(fly ash, slag, silica fume)
Superplasticizers (High-Range Water Reducers) or Water-Reducing Admixtures
Air-Entraining Admixtures
Set-Retarding Admixtures
Set-Accelerating Admixtures

## Slide 16: Concrete Construction Issues
Mix Design
  Proportioning
  Admixtures
Mixing
  Batch plant, Mobile mixing plant
Placing
  Conveyor, Pump, Bucket, Slip-form
Compaction
  Method of vibration, Self-consolidating
Curing
  Membrane curing, Wet-mat curing; Steam curing (in mass-production environments)

## Slide 18: Notes on Concrete Mix Design
Water/cementitious ratio governs strength (0.4~0.5)
Water-reducing admixtures help keep water-cementitious ratio down.

## Slide 20: Concrete Curing
Application of Curing
Compound
Moist-Curing using Wet Cotton Mats

## Slide 22: Portland Cement
I Normal (Ordinary)
II Moderate sulfate resistance
III High early strength
IV Low heat of hydration
V High sulfate resistance

## Slide 23: Measuring Penetration Resistance
Penetrate 1 inch
in 10 seconds
Contact Area
Force Required

## Slide 25
Setting Characteristics of Class P Concrete

## Slide 26: Testing of Fresh Concrete: Slump Test
Low Slump (Low Workability)
High Slump (High Workability)

## Slide 27: Testing of Fresh Concrete Concrete Temperature

## Slide 28: Testing of Fresh Concrete: Air Content
Volumetric Method
Pressure Method

## Slide 29
Approximately 0.01 in

## Slide 30
Notes: The thickness of the protected paste shell is the same for the large and small voids. The total protection is much greater for the smaller voids. We conclude that smaller voids are more efficient at providing frost protection. It is important to recognize, however, that all voids offer frost protection, regardless of size. It is just that the smaller one are more effective relative to their volume. When we have our choice we prefer smaller voids over larger voids. When counting up what we have, however, such as in microscopic analysis of hardened concrete, it is important to include all air voids regardless of size, shape, or origin. (See overhead transparency demo of air void effectiveness.)

## Slide 31: Tests on Hardened Concrete
Compressive
Strength
Split (Indirect)
Tensile Strength
Flexural
Strength
Chloride Permeability
Freeze-Thaw
Resistance
Petrography

## Slide 33: Indirect Tensile Strength

## Slide 34: Asphalt
Asphalt Cement Binder
Asphalt Concete

## Slide 35: Superpave® Binder Classification

## Slide 36: Superpave® Asphalt Binder PG Grading System

## Slide 37: Superpave® Binder Classification Calculated Pavement Temp. in Topeka, KS

## Slide 38: Superpave® Binder Classification PG Binder Grades for Topeka, KS

## Slide 39: Asphalt Concrete: A 3-phase system (aggregate, asphalt cement, air)
Aggregate Solids
Absorbed Asphalt
Effective(free) Asphalt
Air Voids
VAV
VEA
VAGG
VT
MAGG
MAA
MEA
MT
MTA

## Slide 40: Asphalt Concrete Volumetrics: Formulas
VT = VAGG + VEA + VAV; MT = MAGG + MTA = MAGG + MEA + MAA
Specific Gravity of Aggregate = GS; Density of water = W = 1000 kg/m3
Bulk Density of Compacted Mix MB = MT / VT
Theoretical Maximum (Rice) Density MM = MT / (VAGG+VEA)
Bulk Specific Gravity of Compacted Mix GMB = MB / W
Theoretical Maximum (Rice) Specific Gravity of the Mix GMM = MM / W
Total Asphalt Content in Mix = (MTA/MT) * 100
Bulk Volume of Aggregate = Mass of Aggregate/Density = MAGG/(GS * W)
Percent Air Voids (also known as Voids in Total Mix or VTM) = (VAV/VT) *100
%Voids in Mineral Aggregate (VMA) = (Vol. of voids in mix incl. asphalt/VT)*100
= (VAV+VEA)/VT * 100
%Voids Filled with Asphalt (VFA) = VEA/(VAV+VEA) *100

## Slide 41: Schematic of a Hot Mix Asphalt Plant

## Slide 42: Asphalt Concrete Mix Design
Mix design to achieve maximum stability
  Aggregate type & gradation
  Asphalt content (% by weight of total mix)
  % Air voids
Mix design methods
  Marshall Method
  Hveem Method
  Superpave Method

## Slide 43: Marshall Mix Design Method

## Slide 44: SHRP (Superpave®) Gyratory Compactor

## Slide 45: Superpave® Asphalt Concrete Mix Design Criteria

## Slide 46: Superpave® Gyratory Compactor Compaction Curve

## Slide 47: Metals

## Slide 48: Mechanical Properties of Metals
Stiffness - Elastic Modulus or Young’s Modulus (MPa)
Strength - Yield, Ultimate, Fracture, Proof, Offset Yield. Measured as stress (MPa)
Ductility - Measure of ability to deform plastically without fracture - Elongation, Area Reduction, Fracture Strain - (no units or mm/mm)
Toughness, Resilience - Measure of ability to absorb energy (J/m3).
Hardness - Resistance to indentation/abrasion (Various scales, e.g.; Rockwell, Brinell, Vickers.)

## Slide 50: ASTM Tension Test Specimen
2” Gauge Length
Lo

## Slide 51: Raw Data Obtained
Load, P (kN)
Elongation, DL (mm)
Uniform Deformation
Total Elongation
Elastic
Deformation
X
Maximum Load, Pmax
Fracture Load, Pf

## Slide 52: Engineering Stress-Strain Curve
Elongation
0.2% offset
yield stress
Proportional Limit
E
E
(Ultimate)
Engineering Strain, e = DL/Lo
Engineering Stress, S=P/Ao
Sy
Su

## Slide 53
Physical Properties
  Specific Gravity ~ 1.3 to 1.5
  Dry density ~ 20-45 lb/ft3 (300-700 kg/m3)
Mechanical Properties (Extremely anisotropic)
  Young’s Modulus - 1-2 x 106 psi (compression parallel to grain)
  Strength varies widely because of anisotropy, moisture content, defects, etc.
  Tensile strength > compressive strength
  Tensile strength parallel to grain ~20x greater than perpendicular
  10x greater damping than structural metals
Properties of Wood

## Slide 54: The End